## Slide 1
Lubricants
Definition of Lubricants : A substance which is capable of reducing the friction between two surfaces sliding over each other is called Lubricant.
Definition of Lubrication : The process or technique used to reduce the frictional forces between the two sliding and rubbing surfaces of metal are termed as lubrication. The primary objectives of Lubrications are:
To reduce friction between two movin parts.
To minimize wear and tear of moving parts.
To reduce loss of energy in the form of heat by providing cooling effect.
Acts as sealing.
Act as cleaning agent.
To increase the efficiency of the machine by reducing the waste of energy.

## Slide 2
Classification of Lubricants : Lubricants are classified as
Solid Lubricants
Semi –Solid Lubricants
Liquid lubricants
Synthetic Lubricants
Solid Lubricants : Graphite, Molybdenum disulphide, talc,mica etc. are used as solid lubricants. They are generally used in such situation when the operating temperature and pressure is too high and lubricating film is difficult to maintain between the two rubbing surfaces. Solid lubricants are used for railway tract joints, chains, air compressor, open gears , heavy machines etc.

## Slide 3
Synthetic lubricants are used where extreme temperature, chemical reactive atmosphere or some very particular operating conditions are involved Grease is semi solid lubricant. Semisolid lubricant is used where the machine parts are subjected to slow speed, heavy load and sudden jerks and there is a possibility of leaking of lubricant.
Mineral oils,vegetable oils and animal oils are the various types of liquid lubricants. Petroleum based lubricants are included in this category. Liquid lubricants are used in delicate and light machines which work at high speed but under low pressure and where all other lubricants fail to work effectively .

## Slide 4
Synthetic lubricants exhibit greater stability of viscosity with temperature changes, resistance to scuffing and oxidation and fire resistance. Some synthetic lubricants are Phosphate esters, Dibasic acid esters, Silicones, Silicate esters and Polyglycol ether compound.
Lubricating Oils :
Lubricating oils are the substances which not only reduce wear and friction between two moving or sliding metallic surfaces by providing a continuous fluid film in between them, but they also serve as coolant, sealing agents, corrosion preventors etc.

## Slide 5
The most important characteristics of a good lubricating oil are :
1.A high boiling point or low vapour pressure.
2.Suitable viscosity for particular service condition.
3.Low freezing point
4.High thermal stability.
5.High oxidation resistance.
6.Non-corrosive nature
7.Resistance to decomposition at higher or elevated temperatures.
8.High degree of oillness.
There are some properties should be associated with good quality of lubricating oil. They are viscosity, pour point, Flash point, fire point, auto – ignition point, neutralization number, precipitation number, Aniline point etc.

## Slide 6
Viscosity : The viscosity of oil indicates the tendency to resist flow . The viscosity must always be high enough to keep a good oil film between the moving parts. A liquid of high viscosity flows very slowly. The higher the temperature of oil, the lower its viscosity.The variation of viscosity with temperature is known as viscosity index. Lubricating oils are graded by their viscosity index at a certain temperature. The viscosity index (v1) can be represented mathematically as follows.
VL - Vx
V1 = --------------- x 100
VL - VH
VL = standared low viscosity at 1000F
VH = standared high viscosity at 1000F
Vx = viscosity of the oil under test at 1000F
It is observed that oils with high viscosity index is slightly affected by change of temperature.

## Slide 7
Pour point : It is the lowest temperature at which the oil will just cease to flow or pour when cooled under definite prescribed conditions. Thus if an oil is used at a temperature below the pour point , the proper lubrication will not take place. Generally an oil of high viscosity will have a higher pour point than an oil of low viscosity.
Auto ignition point : The temperature at which the flammable vapours given off from the oil will burn.
Neutralisation number : It indicates the acid content in oil and defined as the number of milligrams of KOH required to neutralize 1gm of the oil. An increase in acidic character of oil may affect its quality .The presence of acidic portion of oil will cause deterioration of alloy bearings at elevated temperature.

## Slide 8
Aniline point : It is the specific temperature for an equilibrium solution when equal volume of aniline and lubricating oil is present. A high aniline point indicates higher amount of paraffinic hydrocarbons contents along with lower percentage of aromatic compounds. Low aromatic content is favourable for lubricating oil, as aromatic compounds may dissolve rubbers if present in the oil.
Precipitation Number : It is the measure of the amount of solids or carbon residue contained in the lubricating oil. This number indicates presence of foreign materials in oil. The oil with high precipitation number may cause trouble in oil engine.

## Slide 9
agent include calcium stearate, sodium stearate , lithium stearate fatty acids derivatives and carboxylic acid obtained from castor oil etc. Generally petroleum fractions are used as lubricating oils in the preparation of greases but synthetic oils such as polymerized ethylene oxides, fluorocarbons and siloxanes have also been used.
Silicane grease is polysiloxane –based compound. It does not attack rubber seals and maintain stability under high temperatures. Silicone grease is used with zinc oxide to join heat sink to computer CPUs. Silicone grease is also used in laboratories for lubricating stop cocks and ground glass joints.
Polymer product of tertiary amines ,ethers can be used as synthetic greases after properly fluorinated. They are soft and often used in demanding environments due to their inertness and resistance to oxidation. Fomblin and Krytox are synthetic greases.

## Slide 10
Solid lubricant : There are three general kinds of inorganic compounds that serve as solid lubricants.
a). Layer –lattic solids : These materials have a crystal lattice structure arranged in layers. Graphite, Molybdenum disulphide are commonly employed this class of lubricant. Other materials are tungsten disulphide , mica, boron nitride, borax , silver sulphide etc. Graphite is applied in air compressors, food stuff industry, railway track joints , ball-bearings etc. Molybdenum disulphide used in CV joints and space vehicles

## Slide 12
Polytetrafluoroethylene is typically used as a coating layer on cooking utensils to provide a non stick surface. Its usuable temperature range upto 3500c and chemical intertness make it useful addition in special greases.
b). Soft solids : This class includes a variety of inorganic solids such as white lead, lime, talc, silver iodide and lead monoxide.
C). Chemical coatings: There are many inorganic compounds which can form a metallic surface by chemical reaction. Sulphide, chloride, oxide, phosphate and oxalate films are such examples.
Further films of soft metals (like lead,tin & indium etc) on a hard substance can act as effective solid lubricants.

## Slide 13
Lubricating Emulsions : A dispersion system consisting of two immiscible liquids is called an Emulsions and it is stabilized by adding a third component called emulsifying agent. A well known example of emulsifiers or emulsifying agents is sodium soap (C15H31COONa) .
There are two types of emulsions. These are oil in water emulsion and water in oil emulsions . Oil in water emulsions are obtained by adding an oil to a suitable quantity of water in presence of 3-20 % water soluble emulsifying agent such as sodium soap or sodium and potassium salts of sulphonic acids. These emulsions are used for lubricating cutting tools and pistons in marine diesel engines.

## Slide 14
Water in oil emulsions are prepared by mixing water containing 1-10% water soluble emulsifier (such as calcium stearate ) to the oil and are used to lubricate compressors and provide cooling effect because of evaporation of water, in addition to lubrication.