## Slide 1: FABRIC MANUFACTURE-lll
Weft insertion by Projectile
Weft insertion by Rapier
Weft insertion by Air jet
Weft insertion by other methods
Weaving certain commercial Fabrics
Non-woven Fabrics

## Slide 2: Weft insertion by Water jet- Requirements
Warp and Weft yarns must be water- insensitive ie. Hydrophobic.
All the m/c parts that get wet must of corrosion resistant.
Thermoplastic yarns offer advantage of using heated blade for weft cutting and fused selvedge formation.
Each water jet loom is provided with a miniature pump to feed water under pressure to the nozzle.
A suction slot near the cloth beam is provided in most water jet looms to remove loose water content from the fabric.

## Slide 3: Merits and demerits of water jet loom
Compared to other shuttle less looms ,the water jet loom is least flexible as warp and weft yarns must be water- insensitive ie. Hydrophobic.
Convenient range of fabric is only medium wt. only.
Maximum width of machine is 230 cm.
Best loom for weaving 100% filament fabric production in mass scale.
Hydraulic weft insertion is the lowest energy consuming and least noisy loom.