Fabric Structure & Analysis   I

Class Notes

Chapter 1   The different basic weaves

1.1. Classification of fabrics

The fabrics are classified mainly into three groups .they are

i. Woven fabrics

ii.Knitted fabrics

iii.Non woven farics

Woven fabrics are made by the interlacements of two series threads namely  warp & weft .

Knitted fabrics are made by  knitting  yarn threads in the knitting machine

Non woven fabrics are made by bonding the fibres or yarns by different methods. yarns or fibres are laid in sheet form &bonding  is done mechanically or thermally or chemically.

1.2. Representation  of  weave

The weave is  represented by the interlacement of two series of textile yarn threads named  warp & weft .The interlacement  of warp & weft is taking place at right angles to each other. The warp  is passed above or below the weft or vice versa.

1.3.Use  of Graph paper to represent the design

| 9 |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 8 |  |  |  |  |  |  |  |  |  |
| 7 |  |  |  |  |  |  |  |  |  |
| 6 |  |  |  |  |  |  |  |  |  |
| 5 |  |  |  |  |  |  |  |  |  |
| 4 |  |  |  |  |  |  |  |  |  |
| 3 |  |  |  |  |  |  |  |  |  |
| 2 |  |  |  |  |  |  |  |  |  |
| 1 |  |  |  |  |  |  |  |  |  |
|  | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 |

fig  1 Graph paper

To indicate the order in which the warp & weft  thread interweave to make a fabric , a sort of paper is used called Graph paper which is shown in figure 1.   The paper is ruled in two sets of parallel lines ,crossing the other at right angles , dividing the paper into small rectangular spaces  as shown in figure 1. The vertical rows of graph paper indicates the warp threads & the horizontal ones represents weft thread. Each small square on graph paper  represents a position where a warp & a weft thread  cross one another. A mark put in such small space may mean , according to the idea of designer, a  warp passing over a weft (warp up)  or a weft  crossing over a warp  (weft  up).

In  our case  a mark in the small square indicates the concerned warp is up on concerned weft. A blank in the small square indicates the concerned weft is up on the concerned warp  (the concerned warp is passes below the concerned weft)

1.4.  Definitions

1.4.1 Design-- The processes showing the interlacement of warp & weft in the graph paper is called a design.

1.4.2 Drafting plan-- The processes showing the placement of warps through the male eyes of heald is called a drafting plan.

1.4.3 Lifting plan --The processes indicating the raising or lowering heald shaft during insertion of every weft is called a lifting plan.

1.4.4 Warp--The threads lying parallel to the length of the cloth are called warp. The individual warp is also known as End.

1.4.5-Weft- The threads lying parallel to the width of the cloth are called weft. The individual weft is also known as Pick.

Chapter  2-- Plain weave & its derivatives

2.1. Plain weave Construction

| 2 |  | X |
| --- | --- | --- |
| 1 | X |  |
|  | 1 | 2 |

fig---2  Plain weave

The plain weave is the most elementary weave. It is the combination a combination of two warp threads and two  weft threads interlacing in alternate  order. In this weave every thread in each series passes alternately under and over consecutive threads of the other series uniformly throughout  the fabric . Figure no 2 is representing  plain weave.

2.2 Characteristics of  Plain weave

1. Warp & weft  interlacement takes place in alternate order

2. It has highest nos of binding points

3. Stronger fabric is obtained

4.Yarns in a plain weave fabric are not easily displaced

5.The plain weave fabric tends to be farm and resist slipping

6. Two healds are required to construct a plain weave fabric.

2.3 Derivatives of plain weave

The derivatives of plain  weave are as follows

2.3.1 Regular warp rib

2.3.2 Irregular warp rib

2.3.3 Regular weft rib

2.3.4 Irregular weft rib

2.3.5  Regular matt

2.3.6 Irregular matt

2.3.7 Variegated  matt

| 6 |  | X |
| --- | --- | --- |
| 5 |  | X |
| 4 |  | X |
| 3 | X |  |
| 2 | X |  |
| 1 | X |  |
|  | 1 | 2 |

| 8 |  | X |
| --- | --- | --- |
| 7 |  | X |
| 6 |  | X |
| 5 |  | X |
| 4 | X |  |
| 3 | X |  |
| 2 | X |  |
| 1 | X |  |
|  | 1 | 2 |

2.3.1 Regular warp rib

| 4 |  | X |
| --- | --- | --- |
| 3 |  | X |
| 2 | X |  |
| 1 | X |  |
|  | 1 | 2 |

fig--3  Regular warp rib

fig-4  Regular warp rib

fig-5  Regular warp rib

Regular warp rib weave can be constructed by extending the plain weave vertically. figure 3,4,5 are the examples of regular warp rib where in each case equal extension is taking place. Equal ribs were formed along the  width of the fabric

| 5 |  | X |
| --- | --- | --- |
| 4 |  | X |
| 3 | X |  |
| 2 | X |  |
| 1 | X |  |
|  | 1 | 2 |

| 6 |  | X |
| --- | --- | --- |
| 5 |  | X |
| 4 | X |  |
| 3 | X |  |
| 2 | X |  |
| 1 | X |  |
|  | 1 | 2 |

2.3.2 Irregular warp rib

| 3 |  | X |
| --- | --- | --- |
| 2 | X |  |
| 1 | X |  |
|  | 1 | 2 |

fig--6  Irregular warp rib

fig-7 Irregular warp rib																		fig-8 Irregular warp rib

Irregular warp rib weave can also  be constructed by extending the plain weave vertically. figure 6,7,8 are the examples of   irregular warp rib where in each case  unequal extension is taking place. Unequal ribs were formed along the  width of the fabric.

2.3.3 Regular weft rib

| 2 |  |  | X | X |
| --- | --- | --- | --- | --- |
| 1 | X | X |  |  |
|  | 1 | 2 | 3 | 4 |

| 2 |  |  |  | X | X | X |
| --- | --- | --- | --- | --- | --- | --- |
| 1 | X | X | X |  |  |  |
|  | 1 | 2 | 3 | 4 | 5 | 6 |

| 2 |  |  |  |  | X | X | X | X |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | X | X | X | X |  |  |  |  |
|  | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 |

fig--9  Regular weft rib                         fig--10  Regular weft rib

fig-11  Regular weft rib

Regular weft  rib weave is just opposite warp rib  and  can be constructed by extending the plain weave horizontally. figure 9,10,11 are the examples of regular weft rib where in each case equal extension is taking place. Equal ribs were formed along the  length  of the fabric

2.3.4 Irregular weft rib

| 2 |  |  | X |
| --- | --- | --- | --- |
| 1 | X | X |  |
|  | 1 | 2 | 3 |

| 2 |  |  |  | X | X |
| --- | --- | --- | --- | --- | --- |
| 1 | X | X | X |  |  |
|  | 1 | 2 | 3 | 4 | 5 |

| 2 |  |  |  |  | X | X |
| --- | --- | --- | --- | --- | --- | --- |
| 1 | X | X | X | X |  |  |
|  | 1 | 2 | 3 | 4 | 5 | 6 |

fig--12  Irregular weft rib                         fig--13  Irregular weft rib

fig-14  Irregular weft rib

Irregular weft  rib weave is also constructed by extending the plain weave horizontally. figure 12,13,14 are the examples of regular weft rib where in each case unequal extension is taking place.Unequal ribs were formed along the  length  of the fabric

| 8 |  |  |  |  | X | X | X | X |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 7 |  |  |  |  | X | X | X | X |
| 6 |  |  |  |  | X | X | X | X |
| 5 |  |  |  |  | X | X | X | X |
| 4 | X | X | X | X |  |  |  |  |
| 3 | X | X | X | X |  |  |  |  |
| 2 | X | X | X | X |  |  |  |  |
| 1 | X | X | X | X |  |  |  |  |
|  | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 |

| 6 |  |  |  | X | X | X |
| --- | --- | --- | --- | --- | --- | --- |
| 5 |  |  |  | X | X | X |
| 4 |  |  |  | X | X | X |
| 3 | X | X | X |  |  |  |
| 2 | X | X | X |  |  |  |
| 1 | X | X | X |  |  |  |
|  | 1 | 2 | 3 | 4 | 5 | 6 |

2.3.5  Regular matt

| 4 |  |  | X | X |
| --- | --- | --- | --- | --- |
| 3 |  |  | X | X |
| 2 | X | X |  |  |
| 1 | X | X |  |  |
|  | 1 | 2 | 3 | 4 |

Fig 15 2-2 regular matt

Fig 16 3-3 regular matt

Fig 17 4-4 regular matt

Regular matt can be constructed by extending the plain weave in both vertically & horizontally.  Fig 15 ,16 & 17 are the examples of regular where equal  extension is taking place. Fig 15 ,16 & 17 are known as  2-2, 3-3, &4-4 matt respectively according  to the size of extension.

| 6 |  |  |  |  | X | X |
| --- | --- | --- | --- | --- | --- | --- |
| 5 |  |  |  |  | X | X |
| 4 | X | X | X | X |  |  |
| 3 | X | X | X | X |  |  |
| 2 | X | X | X | X |  |  |
| 1 | X | X | X | X |  |  |
|  | 1 | 2 | 3 | 4 | 5 | 6 |

| 5 |  |  |  | X | X |
| --- | --- | --- | --- | --- | --- |
| 4 |  |  |  | X | X |
| 3 | X | X | X |  |  |
| 2 | X | X | X |  |  |
| 1 | X | X | X |  |  |
|  | 1 | 2 | 3 | 4 | 5 |

2.3.6  Irregular matt

| 3 |  |  | X |
| --- | --- | --- | --- |
| 2 | X | X |  |
| 1 | X | X |  |
|  | 1 | 2 | 3 |

Fig 18 Irregular matt

Fig 19 Irregular matt

Fig 20 Irregular matt

Fig 18 ,19 & 20 are the examples of Irregular  matt .In this case unequal  extension is taking place.

| 8 |  |  |  | X | X | X |  | X |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 7 | X | X | X |  |  |  | X |  |
| 6 |  |  |  | X | X | X |  | X |
| 5 |  |  |  | X | X | X |  | X |
| 4 |  |  |  | X | X | X |  | X |
| 3 | X | X | X |  |  |  | X |  |
| 2 | X | X | X |  |  |  | X |  |
| 1 | X | X | X |  |  |  | X |  |
|  | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 |

| 10 |  |  |  |  | X | X | X | X |  | X |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 9 | X | X | X | X |  |  |  |  | X |  |
| 8 |  |  |  |  | X | X | X | X |  | X |
| 7 |  |  |  |  | X | X | X | X |  | X |
| 6 |  |  |  |  | X | X | X | X |  | X |
| 5 |  |  |  |  | X | X | X | X |  | X |
| 4 | X | X | X | X |  |  |  |  | X |  |
| 3 | X | X | X | X |  |  |  |  | X |  |
| 2 | X | X | X | X |  |  |  |  | X |  |
| 1 | X | X | X | X |  |  |  |  | X |  |
|  | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 |

2.3.7 Variegated  matt

| 6 |  |  | X | X |  | X |
| --- | --- | --- | --- | --- | --- | --- |
| 5 | X | X |  |  | X |  |
| 4 |  |  | X | X |  | X |
| 3 |  |  | X | X |  | X |
| 2 | X | X |  |  | X |  |
| 1 | X | X |  |  | X |  |
|  | 1 | 2 | 3 | 4 | 5 | 6 |

FIG 21 Variegated  matt               FIG 22 Variegated  matt

FIG 23 Variegated  matt

Variegated  matt  can constructed by the  combination of  a regular matt & warp rib & weft rib. Figure 21,22,23 are examples of variegated matt weaves produced from 2-2,3-3,4-4 matt  respectively.

Chapter   3  -Twill weave

3.1 Characteristics of twill weave

The characteristics of twill weave are as follows

1.  Represented by  P/Q  where P-warp float ( warp up) & Q-weft  float(weft up)

2. Number  of ends in a repeat = . Number  of picks in a repeat,R=P+Q

3. Minimum no of ends/picks  required to construct a twill=3

3.  Twill weaves are generally characterised by a series of  more or less  pronounced diagonal wales or ridges &furrows,  with either warp or weft preponderating , or equal quantities, on the face of the fabric.

3.2  Classification of twill weave

3.2.1 Simple balance twill

3.2.2 Warp face twill

3.2.3  Weft face twill

3.2.4 Rearrange twill

3.2.5 Broken twill

3.2.6 Haringbone twill

3.2.7 Zig-zug  twill

3.2.8 Combined twill

3.2.9 Compound twill

| 6 |  |  |  | X | X | X |
| --- | --- | --- | --- | --- | --- | --- |
| 5 |  |  | X | X | X |  |
| 4 |  | X | X | X |  |  |
| 3 | X | X | X |  |  |  |
| 2 | X | X |  |  |  | X |
| 1 | X |  |  |  | X | X |
|  | 1 | 2 | 3 | 4 | 5 | 6 |

3.2.1 Simple balance twill

| 4 |  |  | X | X |
| --- | --- | --- | --- | --- |
| 3 |  | X | X |  |
| 2 | X | X |  |  |
| 1 | X |  |  | X |
|  | 1 | 2 | 3 | 4 |

FIG-24  2/2 twill

FIG-25  3/3 twill

The simple balance twill have equal nos warp float & weft float  (ie P=Q) . figure 24 represents  2up 2down twill (2/2 twill) where each warp is raised continuously for  two times in a repeat. Each  weft is also raised for two times in a  repeat. Similarly in figure 25 each warp & weft raised for three consecutive times.

| 5 |  | X | X | X | X |
| --- | --- | --- | --- | --- | --- |
| 4 | X | X | X | X |  |
| 3 | X | X | X |  | X |
| 2 | X | X |  | X | X |
| 1 | X |  | X | X | X |
|  | 1 | 2 | 3 | 4 | 5 |

3.2.2 Warp face twill

| 3 |  | X | X |
| --- | --- | --- | --- |
| 2 | X | X |  |
| 1 | X |  | X |
|  | 1 | 2 | 3 |

| 4 |  | X | X | X |
| --- | --- | --- | --- | --- |
| 3 | X | X | X |  |
| 2 | X | X |  | X |
| 1 | X |  | X | X |
|  | 1 | 2 | 3 | 4 |

FIG-26  2/1 twill

FIG-27 3/1 twill                                                         FIG-28 4/1 twill

In warp face twill all warps are raised except one during insertion of every pick  in a repeat. These will develop a series of diagonal wales or ridges of warp separated by furrows formed by single stitches of weft . In this case the weft float(Q) is constant & that is one . The warp float(P) may be any number  other than  one. Figure 26,27,28 are the examples of warp face twill design.

3.2.3  Weft face twill

| 5 |  |  |  |  | X |
| --- | --- | --- | --- | --- | --- |
| 4 |  |  |  | X |  |
| 3 |  |  | X |  |  |
| 2 |  | X |  |  |  |
| 1 | X |  |  |  |  |
|  | 1 | 2 | 3 | 4 | 5 |

| 3 |  |  | X |
| --- | --- | --- | --- |
| 2 |  | X |  |
| 1 | X |  |  |
|  | 1 | 2 | 3 |

| 4 |  |  |  | X |
| --- | --- | --- | --- | --- |
| 3 |  |  | X |  |
| 2 |  | X |  |  |
| 1 | X |  |  |  |
|  | 1 | 2 | 3 | 4 |

FIG-29  1/2 twill                              FIG-30 1/3 twill                                                         FIG31- 1/4 twill

In weft face twill  only one  warps is  raised & all others are lowered during insertion of every pick  in a repeat. These will develop a series of diagonal wales or ridges of weft separated by furrows formed by single stitches of warp . In this case the warp float(P) is constant & that is one . The weft float(Q) may be any number  other than  one. Figure 29,30,31 are the examples of weft  face twill design.

3.2.4 Rearrange twill

| 6 |  |  |  | X | X | X |
| --- | --- | --- | --- | --- | --- | --- |
| 5 |  |  | X | X | X |  |
| 4 |  | X | X | X |  |  |
| 3 | X | X | X |  |  |  |
| 2 | X | X |  |  |  | X |
| 1 | X |  |  |  | X | X |
|  | 1 | 2 | 3 | 4 | 5 | 6 |

| 6 |  |  | X |  | X | X |
| --- | --- | --- | --- | --- | --- | --- |
| 5 |  |  | X | X |  | X |
| 4 | X |  | X | X |  |  |
| 3 | X | X |  | X |  |  |
| 2 | X | X |  |  | X |  |
| 1 |  | X |  |  | X | X |
|  | 2 | 1 | 4 | 3 | 6 | 5 |

| 6 |  |  |  | X | X | X |
| --- | --- | --- | --- | --- | --- | --- |
| 5 | X |  |  |  | X | X |
| 4 | X | X |  |  |  | X |
| 3 | X | X | X |  |  |  |
| 2 |  | X | X | X |  |  |
| 1 |  |  | X | X | X |  |
|  | 3 | 2 | 1 | 6 | 5 | 4 |

FIG-32-3/3  twill                                                       FIG-33 Rearrange  twill

FIG-34 Rearrange  twill

Rearrange twill can be produced by altering the ends of a regular twill. Figure 32 is a 3/3 regular twill & from this regular twill the  rearrange twills in figure 33& 34 are derived. In figure  33 the no of ends are rearranged at time is two  ie  ends no 1&2 is exchanged by 2&1  . Similarly 3&4 is exchanged by 4&3, 5&6 is exchanged by 6&5. In figure  34 the no of ends are rearranged at time is three  ie  ends no 1,2&3 is exchanged by3, 2&1  . Similarly 4,5&6 is exchanged by 6,5&4.

3.2.5 Broken twill

Broken twill can be constructed by breaking regular twill. There are two ways to construct a broken twill & they are

3.2.5.1  Rearranging the ends

3.2.5.2 Filling & missing principle

3.2.5.1  Rearranging the ends

| 6 |  |  |  | X | X | X |
| --- | --- | --- | --- | --- | --- | --- |
| 5 |  |  | X | X | X |  |
| 4 |  | X | X | X |  |  |
| 3 | X | X | X |  |  |  |
| 2 | X | X |  |  |  | X |
| 1 | X |  |  |  | X | X |
|  | 1 | 2 | 3 | 4 | 5 | 6 |

| 6 |  |  | X |  | X | X |
| --- | --- | --- | --- | --- | --- | --- |
| 5 |  |  | X | X | X |  |
| 4 |  | X | X | X |  |  |
| 3 | X | X |  | X |  |  |
| 2 | X | X |  |  |  | X |
| 1 | X |  |  |  | X | X |
|  | 1 | 2 | 4 | 3 | 5 | 6 |

FIG-35-3/3  twill                                 FIG-36 Broken twill

| 6 |  |  |  | X | X | X |
| --- | --- | --- | --- | --- | --- | --- |
| 5 |  |  | X |  | X | X |
| 4 |  | X | X |  |  | X |
| 3 | X | X | X |  |  |  |
| 2 | X | X |  | X |  |  |
| 1 | X |  |  | X | X |  |
|  | 1 | 2 | 3 | 6 | 5 | 4 |

FIG-37- Broken twill

This is somewhat similar to rearrange twill. But in this method all ends are not rearranged only   some ends are rearranged  in a repeat.  In figure 36 two ends   from a repeat of 3/3 regular twill are  rearranged ie end no 3&4 in the figure 35 are rearranged by 4&3 .  In figure 37 three  ends   from a repeat of 3/3 regular twill are  rearranged ie end no 4,5 & 6 in the figure 35 are rearranged by6,5&4.

3.2.5.2 Filling & missing principle

| 4 |  |  | X | X |
| --- | --- | --- | --- | --- |
| 3 |  | X | X |  |
| 2 | X | X |  |  |
| 1 | X |  |  | X |
|  | 1 | 2 | 3 | 4 |

|  |  |  | X |  | X | X |  | X |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | X |  |  | X |  | X | X |
|  | X | X |  | X |  |  | X |  |
|  | X |  | X | X |  | X |  |  |
|  | 1 | 2 | 4 | 1 | 3 | 4 | 2 | 3 |

FIG-38- 2/2 regular  twill

FIG-37- Broken twill by " Filling &Missing principle" from 2/2 regular  twill

- Broken twill by " Filling &Missing principle" can be constructed  only from a simple balance twill. In this case any no of ends can be filled & any no of ends can be missed  from a simple balance regular  twill .Generally   half the no of ends in repeat of regular twill is filled  & one less than half the no of ends in repeat of regular twill is missed.  If  R be the  no of ends in repeat of regular twill then

No of ends to be filled ---R/2

No of ends to be missed --(-R/2)-1

No of ends in a repeat of the broken twill  ---R*R/2

FIG-37-  represents  the Broken twill by " Filling &Missing principle" from 2/2 regular  twill . In this case 2 ends are filled 1end is missed& 8 ends will be required for one repeat .

3.2.6 Haringbone twill

| 6 |  |  |  | X | X | X |
| --- | --- | --- | --- | --- | --- | --- |
| 5 |  |  | X | X | X |  |
| 4 |  | X | X | X |  |  |
| 3 | X | X | X |  |  |  |
| 2 | X | X |  |  |  | X |
| 1 | X |  |  |  | X | X |
|  | 1 | 2 | 3 | 4 | 5 | 6 |

| 6 |  |  |  | X | X | X |  |  |  | X | X | X |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 5 |  |  | X | X | X |  | X |  |  |  | X | X |
| 4 |  | X | X | X |  |  | X | X |  |  |  | X |
| 3 | X | X | X |  |  |  | X | X | X |  |  |  |
| 2 | X | X |  |  |  | X |  | X | X | X |  |  |
| 1 | X |  |  |  | X | X |  |  | X | X | X |  |
|  | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 |

FIG-38-3/3  twill                                                     FIG-39- Haringbone twill produced from 3/3  twill

| 4 |  | X | X | X |
| --- | --- | --- | --- | --- |
| 3 | X | X | X |  |
| 2 | X | X |  | X |
| 1 | X |  | X | X |
|  | 1 | 2 | 3 | 4 |

| 4 |  | X | X | X |  |  |  | X |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 3 | X | X | X |  | X |  |  |  |
| 2 | X | X |  | X |  | X |  |  |
| 1 | X |  | X | X |  |  | X |  |
|  | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 |

FIG-40-3/1  twill                                                     FIG41- Haringbone twill produced from 3/1  twill

The haringbone twill is similar to the Broken twill. In this case  the twill line is reversed  in some repeats of the weave throughout the width of the fabric. Straight & Skipped  draft combination is applied  in case of haringbone twill produced from Simple Balance Regular twill &   Straight draft  is applied  in case of haringbone twill produced from  warp face twill . Figure 39 &41 are the examples of haringbone twill. In figure 39 , haring bone twill is constructed  from 3/3 twill. Twill line is reversing  from end no7. The 7th end is the opposite of the 6th end  ( the  "X" mark in the 6th is replaced by blanks in the 7th end. the blanks  in the 6th is replaced by "X"  in the 7th end.) Similarly 8th end is the opposite of the 5th end  ,9th end is the opposite of the 4th end  , 10th end is the opposite of the 3rd end  , 11th end is the opposite of the  2nd  end  & 12th end is the opposite of the  1st end.  By the same procedure haringbone twill  is constructed from 3/1  twill in figure 41.

3.2.7 Zig-zug  twill

Zig-zug  twill can be produced from regular twill . Zig-zug  twill produces  the waviness of  the  twill line . The waviness may be  formed  horizontally or vertically.  To produced waviness,  the regular twill is changing the direction of twill at certain intervals . There are two ways by which the zig-zug twill is formed . They are

3.2.7.1 Horaizental Zig-zug  twill

3.2.7.2 Vertical   Zig-zug  twill

3.2.7.1 Horaizental Zig-zug  twill

| 6 |  |  |  | X | X | X |
| --- | --- | --- | --- | --- | --- | --- |
| 5 |  |  | X | X | X |  |
| 4 |  | X | X | X |  |  |
| 3 | X | X | X |  |  |  |
| 2 | X | X |  |  |  | X |
| 1 | X |  |  |  | X | X |
|  | 1 | 2 | 3 | 4 | 5 | 6 |

FIG-42-3/3  twill

| 6 |  |  |  | X | X | X |  | X | X | X |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 5 |  |  | X | X | X |  |  |  | X | X | X |  |
| 4 |  | X | X | X |  |  |  |  |  | X | X | X |
| 3 | X | X | X |  |  |  | X |  |  |  | X | X |
| 2 | X | X |  |  |  | X | X | X |  |  |  | X |
| 1 | X |  |  |  | X | X | X | X | X |  |  |  |
|  | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 |

FIG-43- Horizontal zig-zug twill produced from 3/3  twill

Horizontal zig zug  twill  produces the waviness  throughout the width of the fabric . To construct             horizontal zig zug  twill  any  even no of  ends  are  selected   for a repeat. The no of picks in a repeat of the        horizontal zig zug  twill  is the same as regular twill.  Generally  the direction of twill will not changed up to  one more than half the no of ends in a repeat .  After that the direction of twill will  changed for the repeat.  If  R0 be the no of  ends  are  selected   for a repeat & R1 no of ends after which the direction of twill  changes.  Then  we have

R1=( R0/2)+1.

Figure -43- represent the Horizontal zig-zug twill produced from 3/3  twill .In this case after 7th no of ends the direction of twill changes as the R0  is 12.

| 12 |  | X | X | X |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| 11 |  |  | X | X | X |  |
| 10 |  |  |  | X | X | X |
| 9 | X |  |  |  | X | X |
| 8 | X | X |  |  |  | X |
| 7 | X | X | X |  |  |  |
| 6 | X | X |  |  |  | X |
| 5 | X |  |  |  | X | X |
| 4 |  |  |  | X | X | X |
| 3 |  |  | X | X | X |  |
| 2 |  | X | X | X |  |  |
| 1 | X | X | X |  |  |  |
|  | 1 | 2 | 3 | 4 | 5 | 6 |

3.2.7.2 Vertical   Zig-zug  twill

| 6 | X | X |  |  |  | X |
| --- | --- | --- | --- | --- | --- | --- |
| 5 | X |  |  |  | X | X |
| 4 |  |  |  | X | X | X |
| 3 |  |  | X | X | X |  |
| 2 |  | X | X | X |  |  |
| 1 | X | X | X |  |  |  |
|  | 1 | 2 | 3 | 4 | 5 | 6 |

FIG-44-3/3  twill

FIG-45- Vertical  zig-zug twill produced from 3/3  twill

Vertical  zig zug  twill  produces the waviness  along  the length of the fabric . To construct   a Vertical zig zug  twill  any  even no of  picks   are  selected   for a repeat. The no of ends  in a repeat of the Vertical  zig zug  twill  is the same as regular twill.  Generally  the direction of twill will not changed up to  one more than half the no of picks in a repeat .  After that the direction of twill will  changed for the repeat.  If  R0 be the no of  picks  are  selected   for a repeat & R1 no of picks   after which the direction of twill  changes.  Then  we have

R1=( R0/2)+1.

Figure -45- represent the Vertical  zig-zug twill produced from 3/3  twill .In this case after 7th no of picks  the direction of twill changes as the R0  is 12.

3.2.8 Combined twill

| 4 |  |  | X | X |
| --- | --- | --- | --- | --- |
| 3 |  | X | X |  |
| 2 | X | X |  |  |
| 1 | X |  |  | X |
|  | A1 | A2 | A3 | A4 |

| 3 |  | X | X |
| --- | --- | --- | --- |
| 2 | X | X |  |
| 1 | X |  | X |
|  | B1 | B2 | B3 |

FIG-46-2/2  twill                        FIG-47-2/1  twill

| 12 |  |  |  | X | X | X | X |  |  | X |  | X |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 11 |  | X | X | X | X |  |  | X |  | X | X |  |
| 10 | X | X | X |  |  | X |  | X | X |  | X | X |
| 9 | X |  |  | X |  | X | X |  | X | X |  | X |
| 8 |  | X |  | X | X |  | X | X |  | X |  |  |
| 7 |  | X | X |  | X | X |  | X |  |  | X | X |
| 6 | X |  | X | X |  | X |  |  | X | X | X | X |
| 5 | X | X |  | X |  |  | X | X | X | X |  |  |
| 4 |  | X |  |  | X | X | X | X |  |  |  | X |
| 3 |  |  | X | X | X | X |  |  |  | X | X | X |
| 2 | X | X | X | X |  |  |  | X | X | X | X |  |
| 1 | X | X |  |  |  | X | X | X | X |  |  | X |
|  | A1 | B1 | A2 | B2 | A3 | B3 | A4 | B1 | A1 | B2 | A2 | B3 |

FIG-48- Combined twill produced from 2/2  & 2/1 twill

Combined  twill is produced from  more than one regular twill. The no of ends/picks in repeat of the combined twill is the LCM of no of ends/picks  in a repeat  of the regular twills taken

3.2.9 Compound twill

Compound twill  is combination two or more regular twills.  Figure no 49 represents the compound twill.

| 6 |  |  | X |  | X | X |
| --- | --- | --- | --- | --- | --- | --- |
| 5 |  | X |  | X | X |  |
| 4 | X |  | X | X |  |  |
| 3 |  | X | X |  |  | X |
| 2 | X | X |  |  | X |  |
| 1 | X |  |  | X |  | X |
|  | 1 | 2 | 3 | 4 | 5 | 6 |

FIG-49- 2,1/1,2 twill

3.2  Diamond Design

There are three types  of  diamond designs . They  are

3.2.1 Weft face diamond

3.2.2  Warp face diamond

3.2.3  Twill base diamond

3.2.1 Weft face diamond

| 10 |  | X |  |  |  |  |  |  |  | X |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 9 |  |  | X |  |  |  |  |  | X |  |
| 8 |  |  |  | X |  |  |  | X |  |  |
| 7 |  |  |  |  | X |  | X |  |  |  |
| 6 |  |  |  |  |  | X |  |  |  |  |
| 5 |  |  |  |  | X |  | X |  |  |  |
| 4 |  |  |  | X |  |  |  | X |  |  |
| 3 |  |  | X |  |  |  |  |  | X |  |
| 2 |  | X |  |  |  |  |  |  |  | X |
| 1 | X |  |  |  |  |  |  |  |  |  |
|  | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 |

Fig-50 : 10 ends  Weft face diamond

For constructing weft face diamond the following steps are performed.

1. Mark out the repeat size in the graph paper

2. Construct a 1/x 'Z'  twill line  starting from bottom of the left hand corner as shown in fig 50

3.  Construct another  1/x  's' twill line starting  from  1square in  or 1 square down of the  top of left  hand corner  as shown in fig 50. Thus weft face diamond is produced

3.2.2 Warp face diamond

| 10 |  | X |  | X | X | X | X | X |  | X |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 9 | X |  | X |  | X | X | X |  | X |  |
| 8 | X | X |  | X |  | X |  | X |  | X |
| 7 | X | X | X |  | X |  | X |  | X | X |
| 6 | X | X | X | X |  | X |  | X | X | X |
| 5 | X | X | X |  | X |  | X |  | X | X |
| 4 | X | X |  | X |  | X |  | X |  | X |
| 3 | X |  | X |  | X | X | X |  | X |  |
| 2 |  | X |  | X | X | X | X | X |  | X |
| 1 | X |  | X | X | X | X | X | X | X |  |
|  | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 |

Fig-51 : 10 ends  Warp face diamond

For constructing weft face diamond the following steps are performed.

1. Mark out the repeat size in the graph paper

2. Construct a 1/x 'Z'  twill line  starting from bottom of the left hand corner as shown in fig 51

3.  Construct another  1/x  's' twill line starting  from  1square in  or 1 square down of the  top of left  hand corner  as shown in fig 51.

4. Now  there are two weft face diamond is produced.  Convert all weft face diamond  into warp face diamond by marking "X" in the squares leaving one  line for  stitch as shown in fig 51.

3.2.3  Twill base diamond

Twill base diamond  is constructed from a  regular twill .  It is constructed on the basis of  of zig zug twill principle. Number ends/picks in a repeat   required to  construct a diamond design  is the even  number  multiple of   number of ends /picks  in a repeat of regular twill  taken.

| 12 |  | X | X | X |  |  |  |  |  | X | X | X |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 11 |  |  | X | X | X |  |  |  | X | X | X |  |
| 10 |  |  |  | X | X | X |  | X | X | X |  |  |
| 9 | X |  |  |  | X | X | X | X | X |  |  |  |
| 8 | X | X |  |  |  | X | X | X |  |  |  | X |
| 7 | X | X | X |  |  |  | X |  |  |  | X | X |
| 6 | X | X |  |  |  | X | X | X |  |  |  | X |
| 5 | X |  |  |  | X | X | X | X | X |  |  |  |
| 4 |  |  |  | X | X | X |  | X | X | X |  |  |
| 3 |  |  | X | X | X |  |  |  | X | X | X |  |
| 2 |  | X | X | X |  |  |  |  |  | X | X | X |
| 1 | X | X | X |  |  |  | X |  |  |  | X | X |
|  | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 |

| 6 | X | X |  |  |  | X |
| --- | --- | --- | --- | --- | --- | --- |
| 5 | X |  |  |  | X | X |
| 4 |  |  |  | X | X | X |
| 3 |  |  | X | X | X |  |
| 2 |  | X | X | X |  |  |
| 1 | X | X | X |  |  |  |
|  | 1 | 2 | 3 | 4 | 5 | 6 |

FIG-52-3/3  twill

FIG-53-Diamond design produced from  -3/3  twill

FIG-53-is the diamond design produced from  -3/3  twill . The following steps are carried out to construct the diamond design

1. Mark out  12 ends & 12 picks in the graph paper.

2.      Construct a horizontal  zig zug twill on the basis of 3/3twill  in the 12ends & first 6 picks as shown in figure 53.

3.  Construct a vertical   zig zug twill on the basis of 3/3twill   in the first 6ends & 12 picks as shown in figure 53.

4. Construct another  vertical   zig zug twill on the basis of 3/3twill   in the last  6ends & 12 picks as shown in figure 53.

3.3 Diaper design

| 12 |  |  |  | X | X | X |  |  |  | X | X | X |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 11 | X |  |  |  | X | X |  |  | X | X | X |  |
| 10 | X | X |  |  |  | X |  | X | X | X |  |  |
| 9 | X | X | X |  |  |  | X | X | X |  |  |  |
| 8 |  | X | X | X |  |  | X | X |  |  |  | X |
| 7 |  |  | X | X | X |  | X |  |  |  | X | X |
| 6 | X | X |  |  |  | X |  | X | X | X |  |  |
| 5 | X |  |  |  | X | X |  |  | X | X | X |  |
| 4 |  |  |  | X | X | X |  |  |  | X | X | X |
| 3 |  |  | X | X | X |  | X |  |  |  | X | X |
| 2 |  | X | X | X |  |  | X | X |  |  |  | X |
| 1 | X | X | X |  |  |  | X | X | X |  |  |  |
|  | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 |

| 6 | X | X |  |  |  | X |
| --- | --- | --- | --- | --- | --- | --- |
| 5 | X |  |  |  | X | X |
| 4 |  |  |  | X | X | X |
| 3 |  |  | X | X | X |  |
| 2 |  | X | X | X |  |  |
| 1 | X | X | X |  |  |  |
|  | 1 | 2 | 3 | 4 | 5 | 6 |

FIG-54-3/3  twill

FIG-55-Diaper  design produced from  -3/3  twill

The diaper design   is constructed from a  regular twill .  It is constructed on the basis of  of haringbone  twill principle. Number ends/picks in a repeat   required to  construct a diaper  design  is the even  number  multiple of   number of ends /picks  in a repeat of regular twill  taken.

FIG-55-is the diaper  design produced from  -3/3  twill . The following steps are carried out to construct the diamond design

1. Mark out  12 ends & 12 picks in the graph paper.

2 Divide the whole repeat into  four equal quarters

3.  Construct a 3/3twill   in the  bottom left hand quarter.

4. Add  "X" marks in 7th end  which is opposite to 6th end . similarly 8th is opposite to5th end, 9th is opposite to 4th end,10th is opposite to 3rd end, 11th is opposite to 2nd  end& 12th is opposite to 1st  end,

5. . Similarly  add  "X" marks also  in 7th pick   which is opposite to 6th pick . similarly 8th is opposite to5th pick, 9th is opposite to 4th pick,10th is opposite to 3rd pick, 11th is opposite to 2nd  pick & 12th is opposite to 1st  pick,

3.4 Satin & Sateen weaves

In  pure sateen & satin weaves the surface of cloth consists  almost entirely either of weft  or warp float ,as in the repeat  of a weave each thread of one series passes over all but one thread of other series  .

In addition , the  interlacing points are arranged as to allow the floating threads to slip and to  cover the' binding '  point  of one thread  by the float of another. This results in the production of fabrics with a maximum degree of smoothness & lustre. The term  " sateen" indicates the weft face construction  & that of "satin"  indicates the warp  face construction  .

The  "sateen " & "satin" weaves are represented by   R/S  where  R is the no of ends/picks in a repeat  or weave no& S is the move no.  The selection of move no (S)  is totally depend upon  the weave no(R).

3.4.1  Selection of move no (S)

The move  number(S)  must not be either one, or one less than the weave number (R), and it must not have a common factor with the weave number. The possible move numbers  for different weave numbers are shown in the table.

Table  1

| Weave number | Move numbers excluded | Possible move numbers |
| --- | --- | --- |
| 5 | 1,4 | 2,3 |
| 6 | 1,2,3,4,5 | none |
| 7 | 1,6 | 2,3,4,5 |
| 8 | 1,2,4,6,7 | 3,5 |
| 10 | 1,2,4,5,6,8,9 | 3,7 |
| 12 | 1,2,3,4,6,8,9 | 5,7 |

3.4.2  Classification of  sateen & satin

3.4.2.1  Weft   face  regular sateen

3.4.2.2  Warp   face  regular satin

3.4.2.3 Irregular sateen

3.4.2.4  4ends & 6ends irregular sattinate

3.4.2.1  Weft   face  regular sateen

| 5 |  |  |  | X |  |
| --- | --- | --- | --- | --- | --- |
| 4 |  | X |  |  |  |
| 3 |  |  |  |  | X |
| 2 |  |  | X |  |  |
| 1 | X |  |  |  |  |
|  | 1 | 2 | 3 | 4 | 5 |

| 5 |  |  | X |  |  |
| --- | --- | --- | --- | --- | --- |
| 4 |  |  |  |  | X |
| 3 |  | X |  |  |  |
| 2 |  |  |  | X |  |
| 1 | X |  |  |  |  |
|  | 1 | 2 | 3 | 4 | 5 |

FIG-56-  5/2 Weft   face  regular sateen

FIG-57-  5/3 Weft   face  regular sateen

FIG-56-  represents the  5 ends Weft   face  regular sateen  by taking the move number  2 & FIG-57-  -  represents the  5 ends Weft   face  regular sateen  by taking the move number  3

3.4.2.2  Warp   face  regular satin

| 5 | X | X | X |  | X |
| --- | --- | --- | --- | --- | --- |
| 4 | X |  | X | X | X |
| 3 | X | X | X | X |  |
| 2 | X | X |  | X | X |
| 1 |  | X | X | X | X |
|  | 1 | 2 | 3 | 4 | 5 |

| 5 | X | X |  | X | X |
| --- | --- | --- | --- | --- | --- |
| 4 | X | X | X | X |  |
| 3 | X |  | X | X | X |
| 2 | X | X | X |  | X |
| 1 |  | X | X | X | X |
|  | 1 | 2 | 3 | 4 | 5 |

FIG-58-  5/2 Weft   face  regular sateen

FIG-59-  5/3 Weft   face  regular sateen

FIG-58-  represents the  5 ends Warp   face  regular sateen  by taking the move number  2 & FIG-59-  represents the  5 ends Weft   face  regular sateen  by taking the move number  3

3.4.2.3 Irregular sateen

| 10 |  |  |  |  |  | X |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 9 |  |  |  |  |  |  |  |  | X |  |
| 8 |  | X |  |  |  |  |  |  |  |  |
| 7 |  |  |  |  | X |  |  |  |  |  |
| 6* |  |  |  |  |  |  |  | X |  |  |
| 5* |  |  | X |  |  |  |  |  |  |  |
| 4 |  |  |  |  |  |  |  |  |  | X |
| 3 |  |  |  |  |  |  | X |  |  |  |
| 2 |  |  |  | X |  |  |  |  |  |  |
| 1 | X |  |  |  |  |  |  |  |  |  |
|  | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 |

FIG 60 -10 ends Irregular sateen

Irregular sateen  can be constructed only for even of  weave numbers .  For constructing   Irregular sateen  the following steps are performed .

1.  Up to half the  number of picks of weave no (R/2) , any  possible   move number  can be taken  say  "s"

2. In one more than  half the number of picks of weave no (R/2+1) ,    move number  in  say  "R/2"

3. In the remaining picks of the weave number , the move number is "R-S"

FIG 60 represents the 10 ends Irregular sateen  where up to 5th pick move number taken is 3. In the 6th pick move number taken is 5. In the remaining picks move number taken is 7.

3.4.2.4  4ends & 6ends irregular sattinate

Although regular sateen cannot be constructed  for 4 &6 end but still irregular sateen is constructed for these ends by varying the move. These designs are known as " sattinate"

| 4 |  |  |  | X |
| --- | --- | --- | --- | --- |
| 3 |  | X |  |  |
| 2 |  |  | X |  |
| 1 | X |  |  |  |
|  | 1 | 2 | 3 | 4 |

| 6 |  |  |  |  |  | X |
| --- | --- | --- | --- | --- | --- | --- |
| 5 |  |  |  | X |  |  |
| 4 |  | X |  |  |  |  |
| 3 |  |  |  |  | X |  |
| 2 |  |  | X |  |  |  |
| 1 | X |  |  |  |  |  |
|  | 1 | 2 | 3 | 4 | 5 | 6 |

FIG 61 -4 ends Irregular sattinate

FIG 61-6 ends Irregular sattinate

Chapter 4. simple towelling & curtain fabric

The  characteristics feature of this weave are alternate raised & sunk diamond- shaped areas which give the effect of honeycomb. Its long floats make it particularly suitable for hand towels, glass cloth, dispensed roller towels &bath mats, where moisture absorption properties are particularly  desired, but in similar coarse cotton qualities it is also used for quilts and soft furnishings, and in finer qualities for shirts and brocades. There are different types of  honeycomb weaves . They are as follows

4.1 Ordinary honey comb

4.2 Ordinary double stitched  honey comb

4.3Straight draft  honey comb

4.4 Brighton honeycomb design

4.1 Ordinary honey comb

| 12 |  | X |  |  |  |  |  |  |  |  |  | X |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 11 |  |  | X |  |  |  |  |  |  |  | X |  |
| 10 |  |  |  | X |  |  |  |  |  | X |  |  |
| 9 |  |  |  |  | X |  |  |  | X |  |  |  |
| 8 |  |  |  |  |  | X |  | X |  |  |  |  |
| 7 |  |  |  |  |  |  | X |  |  |  |  |  |
| 6 |  |  |  |  |  | X |  | X |  |  |  |  |
| 5 |  |  |  |  | X |  |  |  | X |  |  |  |
| 4 |  |  |  | X |  |  |  |  |  | X |  |  |
| 3 |  |  | X |  |  |  |  |  |  |  | X |  |
| 2 |  | X |  |  |  |  |  |  |  |  |  | X |
| 1 | X |  |  |  |  |  |  |  |  |  |  |  |
|  | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 |

| 12 |  | X |  |  |  |  |  |  |  |  |  | X |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 11 | X |  | X |  |  |  |  |  |  |  | X |  |
| 10 | X | X |  | X |  |  |  |  |  | X |  | X |
| 9 | X | X | X |  | X |  |  |  | X |  | X | X |
| 8 | X | X | X | X |  | X |  | X |  | X | X | X |
| 7 | X | X | X | X | X |  | X |  | X | X | X | X |
| 6 | X | X | X | X |  | X |  | X |  | X | X | X |
| 5 | X | X | X |  | X |  |  |  | X |  | X | X |
| 4 | X | X |  | X |  |  |  |  |  | X |  | X |
| 3 | X |  | X |  |  |  |  |  |  |  | X |  |
| 2 |  | X |  |  |  |  |  |  |  |  |  | X |
| 1 | X |  |  |  |  |  |  |  |  |  |  |  |
|  | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 |

FIG 62--   A

FIG 62--    B

For constructing  ordinary honey comb designs ,the steps are performed

1. Construct 1/x twill starting  bottom left hand corner, then a similar one running in opposite direction  and starting  one square in or one square down from the top left hand corner ,so that  there will be a clean intersection of the twill lines as shown at figure 62-A

2.In one of the two diamonds produced, leave a row of stitching points and  then lift the remainder of the diamond solid  as in the figure 62-B

4.2 Ordinary double stitched  honey comb

| 12 |  | X |  |  |  |  |  |  |  | X |  | X |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 11 | X |  | X |  |  |  |  |  | X |  | X |  |
| 10 |  | X |  | X |  |  |  | X |  | X |  |  |
| 9 |  |  | X |  | X |  | X |  | X |  |  |  |
| 8 |  |  |  | X |  | X |  | X |  |  |  |  |
| 7 |  |  |  |  | X |  | X |  |  |  |  |  |
| 6 |  |  |  | X |  | X |  | X |  |  |  |  |
| 5 |  |  | X |  | X |  | X |  | X |  |  |  |
| 4 |  | X |  | X |  |  |  | X |  | X |  |  |
| 3 | X |  | X |  |  |  |  |  | X |  | X |  |
| 2 |  | X |  |  |  |  |  |  |  | X |  | X |
| 1 | X |  |  |  |  |  |  |  |  |  | X |  |
|  | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 |

| 12 |  | X |  |  |  |  |  |  |  | X |  | X |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 11 | X |  | X |  |  |  |  |  | X |  | X |  |
| 10 |  | X |  | X |  |  |  | X |  | X |  | X |
| 9 | X |  | X |  | X |  | X |  | X |  | X | X |
| 8 | X | X |  | X |  | X |  | X |  | X | X | X |
| 7 | X | X | X |  | X |  | X |  | X | X | X | X |
| 6 | X | X |  | X |  | X |  | X |  | X | X | X |
| 5 | X |  | X |  | X |  | X |  | X |  | X | X |
| 4 |  | X |  | X |  |  |  | X |  | X |  | X |
| 3 | X |  | X |  |  |  |  |  | X |  | X |  |
| 2 |  | X |  |  |  |  |  |  |  | X |  | X |
| 1 | X |  |  |  |  |  |  |  |  |  | X |  |
|  | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 |

FIG 63--   A

FIG 63--    B

For constructing  ordinary honey comb designs ,the steps are performed

1. Construct  two  1/x  'Z' twill  one starting from  bottom left hand corner& the other starting  two  square up from bottom left hand corner as shown at figure 63-A   .

2.  Construct  two  1/x  'S' twill  starting  one square in and  one square down from the top left hand corner ,so that  there will be a clean intersection of the twill lines as shown at figure 63-A

3.In one of the two diamonds produced, leave a row of stitching points and  then lift the remainder of the diamond solid  as in the figure 62-B

4.3Straight draft  honey comb

| 12 |  | X |  |  |  |  |  |  |  |  |  | X |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 11 | X |  | X |  |  |  |  |  |  |  | X |  |
| 10 | X | X |  | X |  |  |  |  |  | X |  | X |
| 9 | X | X | X |  | X |  |  |  | X |  | X | X |
| 8 | X | X | X | X |  | X |  | X |  | X | X | X |
| 7 | X | X | X | X | X |  | X |  | X | X | X | X |
| 6 | X | X | X | X |  | X |  | X | X | X | X | X |
| 5 | X | X | X |  | X |  | X |  | X | X | X | X |
| 4 | X | X |  | X |  |  |  | X |  | X | X | X |
| 3 | X |  | X |  |  |  |  |  | X |  | X | X |
| 2 |  | X |  |  |  |  |  |  |  | X |  | X |
| 1 | X |  |  |  |  |  |  |  |  |  | X |  |
|  | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 |

FIG 64-Straight draft  honey comb

FIG 64- represents the Straight draft  honey comb. In this case straight draft is used.

4.4 Brighton honeycomb design

| 12 |  | X | X | X | X | X |  | X | X | X |  | X |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 11 | X |  | X | X | X |  |  |  | X |  | X |  |
| 10* |  | X |  | X |  |  |  |  |  | X |  |  |
| 9* |  |  | X |  | X |  |  |  | X |  |  |  |
| 8 |  | X | X | X |  | X |  | X |  | X |  |  |
| 7 | X | X | X | X | X |  | X |  | X | X | X |  |
| 6 |  | X | X | X |  | X |  | X | X | X | X | X |
| 5 |  |  | X |  | X |  | X |  | X | X | X |  |
| 4* |  |  |  | X |  |  |  | X |  | X |  |  |
| 3* |  |  | X |  |  |  |  |  | X |  | X |  |
| 2 |  | X |  | X |  |  |  | X | X | X |  | X |
| 1 | X |  | X | X | X |  | X | X | X | X | X |  |
|  | 1 | 2 | 3 * | 4 * | 5 | 6 | 7 | 8 | 9 * | 10 * | 11 | 12 |

Fig  65-12 ends  Brighton honeycomb design

For constructing Brighton honeycomb  weave  number  of ends/picks  in a repeat(R) should be  an even  number and  half of the  number  of ends/picks  in a repeat(R)  also should be  an even .  For constructing  Brighton honeycomb weave the  following steps are performed.

1. Mark out the repeat size & divide the repeat into four equal quarters.

2. Mark the centre warp & centre weft in each quarter as shown in the figure 65.

3. Construct  a  1/x  'Z' twill line  starting from the bottom left hand corner.

4. Construct  two   1/x  'S' twill line starting  from  one square in & one square down of the  top  left hand corner.

5. Now add the warp float which is equal to  one less than the half of number of ends/picks in repeat in the centre warps . In our case it is (12/2)-1=5.

6. Now on the basis of these warp floats ,construct warp face diamond.

Chapter  5-yarn numbering systems

Yarn numbering system indicates  the fineness of  yarn .  Whether  the yarn is thick or thin that was decided by the  yarn numbering system. The term  'coarser '  & 'finer'  yarn is used  thick yarn    and  thin yarn . There  are two major systems of yarn numbering system. They are

5.1 Direct system

5.2 Indirect system

5.1 Direct system

The following are the direct yarn numbering  systems.

5.1.1  Tex  count

5.1.2 Danier count

3.1.1  Tex  count---The  tex count is defined as  the   weight  of  one kilometre of yarn  expressed  in gram. If the count of a yarn is 20tex then it indicates that the  weight of 1 kilometre of yarn is 20 gram.

3.1.2 Danier count-- The  danier  count is defined as  the   weight  of  nine  kilometre of yarn  expressed  in gram. If the count of a yarn is 90danier  then it indicates that the  weight of 9 kilometre of yarn is 90 gram.

5.2 Indirect system

The following are the indirect yarn numbering  systems.

5.2.1  English count

5.2.2 Worsted  count

5.2.3 Woollen  count

5.2.1  English count---It is defined as the number of hanks having each hank 840yards contained in one pound. If a yarn have 30s English count then  it indicates that the weight of 30*840 yards  is 1pound  or 30*840 yards contains in 1pound  .

5.2.2 Worsted  count---It is defined as the number of hanks having each hank 560yards contained in one pound. If a yarn have 45s worsted  count then  it indicates that the weight of 30*560 yards  is 1pound  or 30*560 yards contains in 1pound  .

5.2.3 Woollen  count-- It is defined as the number of hanks having each hank 256yards contained in one pound. If a yarn have 50s woollen   count then  it indicates that the weight of 50*256 yards  is 1pound  or 50*256 yards contains in 1pound  .

5.3 Conversion  of one count to another

we have the following  relations among the counts

1.Tex count*English count =590.5

2. Danier count*  English count=5315

3. Worsted count=1.5 * English count

4. Woollen  count=3.3  * English count

5.  1pound=454 gram= 16 ouns=7000 grains

5.4  Resultant count of ply yarns

If multiply yarn  have the individual counts  N1,N2,N3.........then the resultant count  N is given by

1/N= 1/N1  +1/N2 +1/N3............(if the yarn counts are in indirect system)

N= N1  +N2 +N3............(if the yarn counts are in direct system)

example1.   The  weight  of 100meters of yarn was found to be 2gram  .Calculate its count in all direct and indirect system

soln:                 we have

The  weight of 100 meter  = 2 gram

The  weight of 1 meter  = 2/100 gram

The  weight of 1 km(1000 meter  ) = (2/100)* 1000 gram =20 gram

The  weight of 9 km(9000 meter  ) = (2/100)* 9000 gram =180 gram

Counts  are  20tex &180  danier

we have   TEX * English count= 590.5

English count = 590.5/Tex

=590.5/20= 29.25

we have    Worsted count=1.5  * English count= 1.5 * 29.25=43.8

we have    Woollen  count=3.3   * English count= 3.3 * 29.25=96.5

Chapter 6- Heald count & reed count systems

There are  two systems of reed counting

6.1 System based on the number of dents in given space

Table    2

| Name of the system | Basis of numbering |
| --- | --- |
| Stockport | No of dents per 2 inches |
| Radcliff | No of dents per 1 inches |
| Huddersfield | No of dents per 1 inches |
| Metric | No of dents per 1 decm |

6.2 System based on the number of group of  dents in given space

Table    2

| Name of the system | Basis of numbering |
| --- | --- |
| Bolton | No of group of 20 dents per 24.5inches |
| Bradford | No of group of 20 dents per 36 inches |
| Blackburn | No of group of 20 dents per 45 inches |
| Irish | No of group of 100 dents per 40inches |
| Leeds | No of group of 19 dents per 9 inches |
| Macclesfield | No of group of 100 dents per 36 inches |

example  1. What will be the number of ends per inch in a reed of 3/80 stockport

80 stockport = 80 dents per 2 inches

=40 dents per 1 inches

Therefore , no of ends per inch=40 * 3=120

example 2. . What will be the number of ends per inch in a reed of 3/72 bradford

72 bradford = (72 *20)/36 dents per  inches

=40 dents per 1 inches

Therefore , no of ends per inch=40 * 3=120